
FIB Fourier Transform Mask Parameter Table
Saturday, March 19, 2005

Structure details: Integrated multilayer with two reference holes

	Feature
	Final Radius  (μm)

	
	Target
	Actual

	Sample Aperture
	0.75
	

	
	
	

	1st Reference aperture: top
	
	

	1st Reference aperture: bottom
	60nm
	

	2nd Reference aperture: top
	
	

	2nd Reference aperture: bottom
	30nm
	

	Center to center
	3000nm
	


Metal Film Details:
	Front Side
	e4641

	Back Side
	Metallica #7 900nm


Milling Details

	Milling Features
	Outer Radius (μm)
	Inner Radius (μm)
	Ion Beam Current(pA)
	Mag (kX)
	Mill time (s)
	Comments and Filenames

	 Sample
	.78
	0
	15
	35
	35 sec
	Lots of gold possible hillock

	
	.75
	0
	15
	35
	5
	Still gold

	
	.73
	0
	15
	35
	5
	

	
	
	
	
	
	
	Hillocks were a real problem so I made a few small r=.16 holes for 1 second.  These nearly broke through so I made a donut around the structure to try to get some redeposition.

	
	
	
	
	
	
	

	
	
	
	
	
	
	C64_001_overview

	
	
	
	
	
	
	

	
	
	
	
	
	
	

	
	
	
	
	
	
	

	
	
	
	
	
	
	

	
	
	
	
	
	
	

	
	
	
	
	
	
	

	
	
	
	
	
	
	

	
	
	
	
	
	
	

	
	
	
	
	
	
	

	
	
	
	
	
	
	

	
	
	
	
	
	
	

	
	
	
	
	
	
	

	
	
	
	
	
	
	



	Membrane Parameters

Size (μm)
	~125x75

	Thickness (nm)
	100

	Frame size( mm)
	5x5

	Frame thickness (μm)
	200


Dwell: 1.0 μs

Overlap: 50%

Name:  C64	








 Hillocking isn’t worth continuing.  Therefore I have stoped on this one.  











wschlott
Page 1
3/30/2005
E:\data\sample_processing_general\equipment_notes\FIB_guide\FIB_parameter_table.doc

