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Structure details: Integrated multilayer with two reference holes

	Feature
	Final Radius  (μm)

	
	Target
	Actual

	Sample Aperture
	0.5
	D=972x947

	
	
	

	1st Reference aperture: top
	
	D=207x249

	1st Reference aperture: bottom
	60nm
	D=109x106

	2nd Reference aperture: top
	
	D=164x162

	2nd Reference aperture: bottom
	30nm
	D=54x59

	Center to center
	2500nm
	2550


Metal Film Details:
	Front Side
	e4641

	Back Side
	Metallica #7 900nm


Milling Details

	Milling Features
	Outer Radius (μm)
	Inner Radius (μm)
	Ion Beam Current(pA)
	Mag (kX)
	Mill time (s)
	Comments and Filenames

	 Sample
	.55
	0
	13
	35
	20
	Little gold left

	
	.5
	0
	12
	35
	2+2
	

	
	.45
	0
	13
	35
	2
	Gold seems to be gone

	
	
	
	
	
	
	

	1st ref
	.020
	0
	13
	65
	35
	

	2nd ref
	0.020
	0
	13
	65
	18
	

	
	
	
	
	
	
	C62_001_tilt_45_overview

	
	
	
	
	
	
	C62_002_r1

	
	
	
	
	
	
	C62_003_r2

	
	
	
	
	
	
	C62_004_sample_01

	
	
	
	
	
	
	C62_005_sample_02_bright

	
	
	
	
	
	
	C62_006_overview_01

	
	
	
	
	
	
	C62_007_overview_02

	
	
	
	
	
	
	C62_008_overview_03

	
	
	
	
	
	
	C62_009_ot_15kv_overview

	
	
	
	
	
	
	C62_010_pt_r1_round

	
	
	
	
	
	
	C62_011_pt_r2_round

	
	
	
	
	
	
	C62_012_pt_overview

	
	
	
	
	
	
	



	Membrane Parameters

Size (μm)
	~125x75

	Thickness (nm)
	100

	Frame size( mm)
	5x5

	Frame thickness (μm)
	200


Dwell: 1.0 μs

Overlap: 50%

Name:  C62








Image Filenames and Comments


These are very small and very round reference holes.   
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